Supporting Information for

Enhanced Electrochemical Performances of Ni-rich Cathode Materials for Lithium ion Batteries by Mixed Coating Layers

Zunzhi WANG, a,b,*,† Shengxian SHE, a,b,*,† Mengyao LV,b Xujun YUAN,b Hui SUN,b Jun ZHAO,b Jian YU, b and Xufeng YANb

a School of Material Science and Engineering, Zhejiang University, Zheda Road No.38, Hangzhou, Zhejiang, 310000 China

b Ningbo Ronbay New Energy Technology Co., Ltd., Tanjialing East Road No.39 , Ningbo, Zhejiang, 315400 China

Corresponding author: wzz@ronbaymat.com (Z. W.), ssx@ronbaymat.com (S. S.)

†These authors contributed equally to this work.

Figure S1. The SEM images of a), b) NCM9055; c), d) NCM9055-LPO; e), f)

Figure S2. The XPS spectra of a) C 1s, b) O 1s, c) Li 1s, d) Al 2p, e) B 1a, and f) P 2p.

Figure S3. The XRD of cycled NCM9055, NCM9055-LPO, and NCM9055-LPB.

Figure S4. The SEM of cycled NCM9055, NCM9055-LPO, and NCM9055-LPB.

Table S1. The physical and chemical properties of NCM9055, NCM9055-LPO, and NCM9055-LPB.

| Samples | Items | Unit | NCM9055 | NCM9055-LPO | NCM9055-LPB |
| --- | --- | --- | --- | --- | --- |
| Physical &Chemical Properties | Li | wt % | 7.23 | 7.24 | 7.22 |
|  | Ni | wt % | 90.27 | 90.30 | 90.31 |
|  | Co | wt % | 5.03 | 4.98 | 4.79 |
|  | Mn | wt % | 4.70 | 4.72 | 4.90 |
|  | Li2CO3 | wt % | 1.1035 | 0.1082 | 0.2444 |
|  | LiOH | wt % | 0.5592 | 0.2432 | 0.2550 |
|  | BET | m2/g | 0.2991 | 1.1127 | 0.3846 |
|  | pH |  | 12.07 | 11.38 | 11.20 |
|  | Dmin | μm | 4.78 | 4.80 | 4.78 |
|  | Dmax | μm | 21.67 | 21.65 | 21.65 |
|  | D50 | μm | 10.38 | 10.42 | 10.21 |
|  | (D90-D10)/D50 | - | 0.67 | 0.67 | 0.67 |
| Coin cell (4.25~2.5V) | 0.2C-rate Charge | mAh/g | 230.6 | 230.3 | 235.6 |
|  | 0.2C-rate Dis. | mAh/g | 200.9 | 206.9 | 213.4 |
|  | Eff. | % | 87.1 | 89.8 | 90.6 |