## Slide 1
High-Performance Nickel-Based Electrodes in State-of-the-Art Lithium-Ion Batteries: Morphological Perspectives
Agus Purwanto, Shofirul Sholikhatun Nisa, Ike Puji Lestari, Muhammad Nur Ikhsanudin Cornelius Satria Yudha, and Hendri Widiyandari
CENTRE OF EXCELLENCE FOR ELECTRICAL ENERGY STORAGE TECHNOLOGY, SEBELAS MARET UNIVERSITY
www.puibaterai.uns.ac.id

## Slide 2
Nickel as the Future of Energy Storage
Effect of morphology toward the performance of materials

## Slide 3
Table of Content
Introduction
01
Particle Morphology for Nickel-Based Anode Materials
02
Precursors for Nickel-Rich Cathode Materials
03
Nickel-Rich Cathode Materials
04
Current Advances and Future Projections
05
Conclusion
06

## Slide 4
High abundancy Transitional Metal
Nickel has Good Redox Ability
Excellent Choice for Electrochemical Purposes
Nickel as a versatile material
Introduction : “Unravelling Ni Potential”

## Slide 5
Introduction : “Nickel as Secondary Energy Storage”
Lead Acid Batteries
Nickel Cadmium Batteries (NiCd)
Nickel Metal Hydride (Ni-MH)
Li-ion Batteries (LIBs)
Higher Gravimetric and
Volumetric Density
Higher Energy Density
Higher Power Density

## Slide 6
Introduction : “Development of Nickel Based Batteries”
BCG research ; BCG Article “Batteries for ElectricCars” (2010)

## Slide 7
Introduction : “Development of Cell Chemistry in Li-ion Batteries”

## Slide 8
Introduction : “an alternative for carbonaceous anode material”
Ni Based Anodes
Metallic Nickel
Nickel Oxides
Nickel Hydroxide
Nickel Sulfide
Nickel Oxalate
Derivate of Nickel Oxides
Potential alternative for graphite anode
Conversion/ Alloying type of Anode
High theoretical or initial Li storage
Suffers from low efficiency
Can be enhanced by modification

## Slide 9
Particle Morphology for Nickel-Based Anode Materials
Nano-sheets
Nano-flakes
Nano-plates
Nano-rods
Nano-spikes
Urchin/Flower like
(a) Nano-spike morphology of NiS material, reprinted with permission from Ref. (Sonia et al., 2014) Copyright (2014) Elsevier B.V. (b) NiS flower-like particle, reprinted with permission from Ref. (Ma et al., 2015) Copyright (2015) Springer Nature Limited, (c) NiS Urchin-like particle, reprinted with permission from Ref (Mi et al., 2013) Copyright (2013) RSC Publishing.

## Slide 10
Particle Morphology for Nickel-Based Anode Materials
Unique Morphology :
High surface area
Better electron and ion transport
Improved conductivity
Prone to particle expansions
Better Thermal stability
Easily modified by using functional materials

## Slide 11
Ni-based Materials | Methods | Modification | Morphological feature | Electrochemical Performance (Capacity/Cycle/Rate) | Reference
Ni(OH)2 | Precipitation | - | Ultra-thin nanosheet | 2019/1358 mAh g−1/0.1 C | (Yanwei Li et al., 2017)
Ni(OH)2 | Precipitation | Al-doping 20% w/w | Nanosheet | 681 mAh g−1/30 cycles/0.1 C | (Li et al., 2016)
Ni(OH)2 | Hydrothermal | Ni(OH)2/delaminated-Ti3C­2 | Nanosheet | 121 mAh g−1/1000 cycles/0.1 C | (C. Li et al., 2020)
Ni-Co-hydroxide | Hydrothermal | Combine Co-Ni hydroxide | Nanosheet | 373 mAh g−1/500 cycles/0.1 C | (Shi et al., 2017)
Ni(OH)2 | One-step in-situ polymerization | GO/PANI blending | Nanosheet | Capacity fading 15.6% after 2000 cycles | (Ma et al., 2016)
Ni(OH)2 | precipitation | rGO blending | Nano-flakes | 1500/40 cycles/0.1 C | (Zhu et al., 2014)
NiO | CLD and graft growth under air condition | - | Nano-flakes | 1.94 mAh cm−2/140 cycles/0.1 C | (Ni et al., 2013)
NiO | CBD | - | Nano-flakes | 700 mAh g−1/50 cycles/0.1 C | (Huang et al., 2009)
NiO | Hydrothermal | Graphene blending | Nanoplate | 1318 mAh g−1/100 cycles/0.1 C | (Du et al., 2018)
NiS | Hydrothermal | Cladding carbon (C-NiS) | Flake-shape | 575.4 mAh g−1/30 cycles | (Wang et al., 2013)
NiS/G (1 : 1) | Hummers method continued with thermal reduction | Mass ratio NiS to graphene | Nanosheet | 887 mAh g−1/60 cycles/0.1 C | (Geng et al., 2014)
NiS/G (2 : 1) | Hummers method continued with thermal reduction | Mass ratio NiS to graphene | Nanorod | 458 mAh g−1/60 cycles/0.1 C | (Geng et al., 2014)
NiS | Solvothermal | Reactant concentration | Nanorod | 670 mAh g−1/100 cycles | (Long et al., 2016)
NiS | Hydrothermal | Reaction time (24 h) | Nano-spike | 550 mAh g−1/100 cycles/0.1 C | (Sonia et al., 2014)
Camphoric carbon wrapped -NiS | Hydrothermal | Addition of camphoric carbon | Nano-spike | 550 mAh g−1/100 cycles/0.1 C | (Sebastian et al., 2014)
NiS | Hydrothermal | CTAB assistant | Flower-like | 6733 mAh g−1/10 cycles | (Ma et al., 2015)
NiS | Solvothermal | Nickel complex precursor | Urchin-like | 597.3 mAh g−1 | (Mi et al., 2013)
NiC2O4. 2H2O | Hydrothermal | Reaction temperature | Nanorod | 1109 mAh g−1 | (Oh et al., 2016)
Preparation of Ni-based particle for anode material of Li-ion batteries

## Slide 12
Precursors for Nickel-Rich Cathode Materials : Types
Hydroxides
Carbonates
Oxalates
Oxides
Salts (Nitrates, Acetates, etc)

## Slide 13
Precursors for Nickel-Rich Cathode Materials : Morphology
Nano-sheets Primary Particles
Nano-flakes Primary Particles
Nano-plate Primary Particles
Nano-Rods Primary Particles
Needle-Like Primary particles

## Slide 14
Precursors for Nickel-Rich Cathode Materials : Morphology
(a) Nanosheet primary particle of NMC-based material, reprinted with permission from Ref. (Fu et al., 2014) Copyright (2014) ACS Publications, (b) Nanoflake primary particle of NMC-811 cathode material, reprinted with permission from Ref. (Mo et al., 2020) Copyright (2020) Elsevier B.V., (c) Nanoplate primary particle of NCA cathode material, reprinted with permission from Ref. (Q. Wang et al., 2018) Copyright (2018) Electrochemical Science Group, (d) Nanorod primary particle of NMC cathode material, reprinted with permission from Ref. (Sun et al., 2019) Copyright (2019) ACS Publications, (e) Needle-like particle of NCA-material, reprinted with permission from Ref. (Duan et al., 2018) Copyright (2018) Elsevier B.V.

## Slide 15
Nickle-rich cathode precursors and their morphology
Precursors | Metal Sources/ modification | Methods | Temperature (oC)/Time/ Condition | Morphological feature | Reference
NMC-OH | Nitrates | solvothermal | 160 | Nanosheet | (Fu et al., 2014)
NMC-811-OH | Sulfates | precipitation |  | Nano-flake | (Mo et al., 2020)
NCA | Ni-Co-Li-acetate Al-nitrate | Sol-gel | 85/8 h stirring | Nanoplate | (J. Li et al., 2020)
NMC-622 | Ni-Co-nitrate Mn-Mn(Ac)2 | Ammonia-induced and coprecipitation | 96/6 h ammonia evaporation | Nanoplate | (Liu et al., 2016)
NMC-7 1.5 1.5 | Acetate | Hydrothermal | 150/4 h process | Nanoplate | (Tian et al., 2016)
NMC-622 | Sulfate | Coprecipitation | - | Nanorod | (Yang et al., 2019)
NMC-FCG | Sulfate/NMC-532 solution added into NM-73 solution | Coprecipitation |  | Nanorod | (Noh et al., 2014)
NCA-OH | Commercial precursor-NH4H2PO4 combined | - |  | Needle-like | (Tang et al., 2017)
Al-doped-NCA | Sulfate/Al doping | Coprecipitation |  | Needle-like | (Duan et al., 2016)
NCA | Ni-Co-OH with addition of Al-nitrate |  | 60/500 rpm/CO2 condition | Needle-like | (Duan et al., 2018)
NCW | Ni-Co-sulfate/replacement of Al with W | precipitation | Inert (N2) condition | Needle-like | (Ryu et al., 2019)
NMC-811 | Commercial precursor + PVP | Pre-oxidized process | 40 | Needle-like | (Zhang et al., 2018)
NMC-811 | Sulfate | Solid state with controlled crystallization | 50 | Needle-like | (G. Yang et al., 2020)
Al-doped-NMC-811 | Commercial precursor/Al doping from nitrate source |  | 80/sol phase | Needle-like | (Du et al., 2021)

## Slide 16
Nickel-Rich Cathode Materials : Primary vs Secondary Particles
Secondary Particles
Primary Particles

## Slide 17
Nickel-Rich Cathode Materials : Types
Layered
NMCs
Spinel
LiNi1.5Mn0.5O4
NCA
LNO (LiNiO2)
Olivine
LiNiPO4
LiNi1-xMxPO4

## Slide 18
Nickel-Rich Cathode Materials : Primary Particle Morphology vs Electrochemical Properties
Material | Precursor/ modification | Morphological feature | Electrochemical Properties (Capacity/Cycle/Rate) | Reference
NMC-811 | NMC-811-OH/modified coprecipitation and solid-state | Nanosheet | 195 mAh g−1/300 cycles/0.1 C | (Xu et al., 2019)
NMC-811 | NMC-OH/modification of ammonia concentration controlled | Nanosheet | 201 mAh g−1/100 cycles/0.2 C | (Su et al., 2018)
NMC-7 1.5 1.5 | NMC precursor with solvothermal method | Nanosheet | 184.7 mAh g−1/100 cycles/0.1 C | (Fu et al., 2014)
NMC– 8.5 0.75 0.75 | NMC precursor with hydrothermal method | Nanosheet | 189.5 mAh g−1/300 cycles/0.2 C | (Liu et al., 2019)
NMC-811 | NMC-OH/TiO2 doping | Nano-flake | 258 mAh g−1/150 cycles/1 C | (Mo et al., 2020)
NCA | NCA-OH | Nano-flake | 210.4 mAh g−1/40 cycles/0.1 C | (Q. Wang et al., 2018)
NMC-622 | NMC-OH | Nanoplate | 173 mAh g−1/100 cycles/0.2 C | (Liu et al., 2016)
NMC-622 | NMC-OH | Nanorod | 193.6 mAh g−1/300 cycles | (Yang et al., 2019)
NMC-6 2.5 1.5 | Combination of NMC-7 2.5 0.5-OH and NMC-5.8 2.5 1.7-OH | Rod-shape | 206 mAh g−1/1000 cycles | (Noh et al., 2013)
NMC-5.4 3 1.6 | Modification of Ni/Mn/Co concentration gradient (FCG) | Nanorod | 183.7 mAh g−1/100 cycles | (Noh et al., 2014)
NCA-8.15 1.5 0.35 | NCA-OH/NH4H2PO4 doping | Needle-like | 195.3 mAh g−1/200 cycles/0.1 C | (Tang et al., 2017)
NCA-8.15 1.5 0.35 | NCA-OH/Al-gradient-doped | Needle-like | 187.5 mAh g−1/200 cycles | (Duan et al., 2016)
NCA-9 0.7 0.3 | NCA-OH/Al-doped | Needle-like | 224.6 mAh g−1/100 cycles | (Duan et al., 2018)
NCW-9 0.9 0.1 | NCW-OH/Replacing Al with W | Needle-like | 231.2 mAh g−1/200 cycles/0.1 C | (Ryu et al., 2019)
NCA | Pre-oxidized method | Needle-like | 175 mAh g−1/100 cycles | (Zhang et al., 2018)
NCA | Solid state with controlled crystallization | Needle-like | 187.7 mAh g−1/100 cycles | (G. Yang et al., 2020)
NCA | Al-doping | Needle-like | 171.4 mAh g−1/1000 cycles/1 C | (Du et al., 2021)

## Slide 19
Nickel-Rich Cathode Materials : Secondary Particles
Microsphere/Spherical
Quasi/Pseudo Spherical
Hollow Spherical
Non-spherical/
Agglomerated

## Slide 20
Cathode materials | Methods | Chelating agents/ Additives | Morphological feature | Electrochemical Performance (Capacity/Cycle/Rate) | Reference
NCA | Coprecipitation | Ammonia | Dense spherical particles, 5–12 µm | 196 mAh/g/95% after 50 cycles/150 mAh/g at 2 C | (Hu et al., 2012)
 | Coprecipitation | Ammonia | Dense spherical particle, 4–6 µm | 206 mAh/g/80% after 50 cycles at 55 ℃/~130 mAh/g at 5 C 55 ℃ | (Kim et al., 2014)
 | Coprecipitation | 5-sulfosalicylic acid | Dense spherical particles, ~4–8 µm | 203 mAh/g/90% after 200 cycles at 1 C/174 mAh/g at 1 C | (Xie et al., 2015)
 | Coprecipitation | EDTA | Dense spherical particles, ~10 µm | 193 mAh/g/90% after 100 cycles at 1 C/- | (Xie et al., 2016)
 | Coprecipitation | Ammonia | Dense spherical particles, ~10 µm | 183 mAh/g/91% after 100 cycles at 1 C/140 mAh/g at 5 C | (Seo and Lee, 2017)
 | Spray Pyrolysis | Citric acid-Ethylene glycol-DCCA | Spherical particles, ~1 µm | 218 mAh/g/100% after 20 cycles at 0.1 C/- | (Ju et al., 2010)
 | Spray pyrolysis |  | Spherical/yolk shell particles, 1.1–1.6 µm | 225 mAh/g/89% after 49 cycles at 0.2 C/129 mAh/g at 1 C | (Yang et al., 2014)
 | Flame spray pyrolysis | Urea | Quasi-spherical | 124 mAh/g/81% after 200 cycle at 0.5 C/- | (Nurcahyani et al., 2020)
 | Spray drying | Glycerol | Spherical, 10–20 µm | 200 mAh/g/91% after 200 cycles at 1 C/130 mAh/g at 5 C | (J. Zhang et al., 2020)
 | Spray drying | Citric acid | Spherical and hollow particles, 10–50 µm | 188 mAh/g/94% after 100 cycles at 0.5 C/- | (Park and Chan Kang, 2014)
NMC622 | Coprecipitation | Ammonia | Dense spherical particles, 10–20 µm | 172 mAh/g/94% after 100 cycles at 1 C/143 mAh/g at 10 C | (Liang et al., 2014)
 | Coprecipitation | Sodium Lactate | Quasi-spherical particles, ~4 µm | 201 mAh/g/78% after 100 cycles at 0.1 C/~120 mAh/g at 5 C | (Xu et al., 2018)
 | Coprecipitation | Ammonia | Quasi-spherical particles, <8 µm | 155 mAh/g/96% after 30 cycles at 0.5 C/- | (Fu et al., 2011)
 | Coprecipitation | Ammonia | Quasi-spherical particles, <1.2 µm | 186 mAh/g/95% after 10 cycles at 0.5 C/~50 mAh/g at 5 C | (Ronduda et al., 2020)
 | Sol-gel | Citric acid | Spherical particles, 800 nm | 174 mAh/g/87% after 100 cycles at 1 C/~70 mAh/g at 10 C | (Lee et al., 2016)
 | Spray pyrolysis |  | Spherical particles, 5–13 µm | - | (Tian et al., 2018)
NMC7 1.5 1.5 | Coprecipitation | Ammonia | Dense spherical particles, 6–21 µm | 185 mAh/g/95% after 50 cycles at 0.2 C/- | (Lu et al., 2014)
 | Coprecipitation | Ammonia | near-spherical particles, 200–500 nm | 164 mAh/g/-/- | (Zhang et al., 2012)
NMC712 | Sol-gel | Citric acid | Quasi-spherical with 300–800 nm primary particle | 205 mAh/g/86.24% after 100 cycles/137 mAh/g at 5 C | (Dong et al., 2019)

## Slide 21
Cathode materials | Methods | Chelating agents/ Additives | Morphological feature | Electrochemical Performance (Capacity/Cycle/Rate) | Reference
NMC811 | Coprecipitation | Ammonia | Dense spherical particles, 14–16 µm | 202 mAh/g/96% after 200 cycles at 1 C/~54 mAh/g at 10 C | (Duan et al., 2020)
 | Coprecipitation | Ammonia + NH4F | Dense spherical particles, ~10 µm | 202 mAh/g/94% after 100 cycles at 2 C/~141 mAh/g at 10 C | (Yue et al., 2013)
 | Coprecipitation-Spray Dry | Ammonia | Dense spherical particles, ~12 µm | ~175 mAh/g/86% after 100 cycles at 1 C/~130 mAh/g at 10 C | (Huang et al., 2019)
 | Flame spray pyrolysis |  | Spherical particles, 1 µm | 178 mAh/g/85% after 25 cycles at 1 C/- | (Abram et al., 2019)
 | Hydro/ Solvothermal | Ethylene glycol | Spherical particles, 6–8 µm | 201 mAh/g/81% after 100 cycles at 0.1 C/142 mAh/g at 10 C | (Gu et al., 2021)
 | Spray pyrolysis |  | Submicron particles from spherical particle breakage | 197 mAh/g/93% after 80 cycles at 1 C/173 mAh/g at 5 C | (Yan Li et al., 2017)
NFA F=Fe | Coprecipitation | Ammonia | Spherical particle, ~8–10 µm | 190 mAh/g/88% after 30 100 cycles at 0.33 C/110 mAh/g at 1 C | (Muralidharan et al., 2020)
LNMO | Coprecipitation | Ammonia | Spherical particle, ~10 µm | ~220 mAh/g/86% after 100 cycles at 0.5 C/~145 mAh/g at 10 C | (Sun et al., 2013)
 | Coprecipitation | Ammonia | Spherical particle, ~3 µm | 197 mAh/g/94% after 100 cycles at 0.2 C/- | (Ma et al., 2020)
LNO | Coprecipitation | Ammonia | Spherical particle | 216 mAh/g/80% after 200 cycles at 1 C/121 mAh/g at 5 C | (Mu et al., 2020)

## Slide 22
Nickel-Rich Cathode Materials : Microcracking of Agglomerated Particles
(a,b) Silkworm like NMC811 particles before cycles and (c) after 100 cycles, reprinted with permission from Ref. (Lei et al., 2019b) Copyright (2019) Elsevier B.V
Microcracking :
Disintegration of Secondary Particle
Caused by expansion-shrinkage of particles during insertion and deinsertion of Li ions
Resulting in rapid capacity decay due to : excessive electrolyte exposure and passivation layer formation

## Slide 23
Nickel-Rich Cathode Materials : Single Crystal Particle (Solution to Microcracking)
Morphology distribution in single crystal NMC. SEM images of (a) precursor and (b, c) sintered single crystal NMC, reprinted with permission from Ref. (Fan et al., 2020) Copyright (2020) Elsevier B.V.

## Slide 24
Nickel-Rich Cathode Materials : Single Crystal Particle (Solution to Microcracking)
Sample | Synthesis Method | Precursor | T (°C) | Particle Size (µm) | Specific Capacity | Ref.
NMC 761410 | Coprecipitation and molten salt | Hydroxide precursor | 900 | 3 | 182.3 mAh/g at 0.1 C | (Bi et al., 2020)
NMC 811 | Coprecipitation | Hydroxide precursor | 740 | - | 197.9 mAh/g at 0.1 C | (Xu et al., 2019)
NMC 811 | Spray pyrolysis | Oxide precursor | 900 | 1–5 | 211 mAh/g at 0.1 C | (Zhu et al., 2020)
NMC 811 | Coprecipitation or molten salt |  | 850 | 1 | - | (Zhu and Chen, 2019)
NMC 811 | Coprecipitation | Hydroxide precursor | 830 | 1–4 | - | (C. Yang et al., 2020)
NMC 811 | Commercial | Hydroxide precursor | 800–960 | 1–1.5 | 194 mAh/g at 0.1 C | (Zhao et al., 2019)
NMC 910603 | Coprecipitation | Hydroxide precursor | 820 | 1–2.5 | 203.8 mAh/g at 0.1 C | (Lee et al., 2020)
NCA 880903 | Coprecipitation | Hydroxide precursor | 840 | 4–5 | 240 mAh/g at 0.1 C | (H. Zhang et al., 2020)
Single crystal nickel-rich cathode materials

## Slide 25
Nickel-Rich Cathode Materials : Comparison
The Morphology of Pre Cycle and Post Cycling of Nickel Rich Cathode Material : the effect of morphology of nickel-rich cathode towards its likability to pulverized during the prolonged charge-discharge process

## Slide 26
Overcoming the Capacity Fading and Improving the Electrochemical
Properties of Nickel Based Cathode
Development of Multilayer Particles
PROTECTIVE NANO-COATINGS
Development of Porous Materials
nanospheres
Nano-tubes
Nano-rods
Cathode A
Cathode B
Cathode C
Current Advances and Future Projections

## Slide 27
Conclusion
Nickel Has Been Utilized as the Main Component for Li-ion Batteries Electrodes (Anode and Cathodes)
Several studies have been employed to improve the electrochemical performance of active materials via morphology engineering/tailoring
Future studies should focus on the development of long-lasting nickel-based Li-ion batteries
The morphology of nickel-based active materials is one of the major determining factors for high-performance Li-ion batteries.

## Slide 28
This paper is supported by Indonesia Endowment Fund for Education (LPDP / Lembaga Pengelola Dana Pendidikan) through Pendanaan Riset Inovatif Produk (Rispro) Invitasi grant no.PRJ-6/LPDP/2020
THANK YOU