Supporting Information

Operando Observation of Lithiation and Delithiation Reactions of a LiCoO2 - Li3BO3 Composite Electrode Formed on a Li6.6La3Zr1.6Ta0.4O12 Solid Electrolyte Sheet by Laboratory-based Hard X-ray Photoelectron Spectroscopy

Tsukasa IWAMA1,2,§, Tsuyoshi OHNISHI2,*, and Takuya MASUDA1,2,*,§§

- Graduate School of Chemical Sciences and Engineering, Hokkaido University, Kita 13, Nishi 8, Kita-ku, Sapporo, Hokkaido 060-0810, Japan

- Research Center for Energy and Environmental Materials, National Institute for Materials Science (NIMS), 1-1 Namiki, Tsukuba, Ibaraki 305-0044, Japan

- Corresponding author: Masuda.Takuya@nims.go.jp and OHNISHI.Tsuyoshi@nims.go.jp

§ ECSJ Student Member

§§ ECSJ Active Member

ORCID:
Tsukasa IWAMA: 0000-0002-1453-6936

Tsuyoshi OHNISHI: 0000-0002-2333-7752

Takuya MASUDA: 0000-0001-7462-2177

Estimation of amount of LBO

LBO is formed by mixing 10 μL of aqueous solutions saturated with LiOH and H3BO3, followed by annealing, according to the following chemical reaction:

3LiOH+H3BO3→Li3BO3+3H2O

The moles of LiOH (saturation solubility: ~5.22 mol/L) and H3BO3 (saturation solubility: ~0.94 mol/L) contained in the 10 μL of saturated aqueous solutions are 5.22 × 10-5 mol and 9.38 × 10-6 mol, respectively. Thus, the amount of Li3BO3 (79.634 g/mol) can be roughly estimated to be 9.38 ×10-6 mol (0.747 mg).

Figure S1 (a) A SEM image and (b) EDS map of LCO-LBO composite positive electrode in top view.

Figure S1 shows a SEM image and EDS map of the LCO-LBO composite positive electrode. The size of primary LCO particles is around 200 nm and those are interconnected by LBO distributed in the composite positive electrode

Figure S2 Cross-sectional (a, c, e) SEM images and (b, d) EDS maps of the LCO-LBO composite positive electrode. (a, b) The top side (outermost side), (c, d) bottom side (LLZT side) and (e) entire LCO-LBO composite electrode.

Figure S2 shows cross-sectional SEM images and EDS maps of the LCO-LBO composite positive electrode. LBO is well distributed in the entire composite electrode but some LBO is segregated on the top and bottom of the composite electrode.

Figure S3  (a) Co 2p3/2, (b) B 1s, (c) C 1s, and (d) Li 1s photoelectron spectra of the LCO-LBO composite electrode before and after charge/discharge cycles without calibration.

Figure S4 (a) Co 2p3/2, (b) B 1s, (c) C 1s, and (d) Li 1s photoelectron spectra of the LCO-LBO composite electrode before and after charge/discharge cycles with calibration using the Co 2p peak of LCO at 780.0 eV.

Figure S5 (a) Co 2p3/2, (b) B 1s, (c) C 1s, and (d) Li 1s photoelectron spectra of the LCO-LBO composite electrode before and after charge/discharge cycles with calibration using the B 1s peak of LBO at 191.5 eV.

Figure S6 (a) Co 2p3/2, (b) B 1s, (c) C 1s, and (d) Li 1s photoelectron spectra of the LCO-LBO composite electrode before and after charge/discharge cycles with calibration using the C 1s peak of hydrocarbon at 285.0 eV.

|  |  | Without asymmetry | With asymmetry |
| --- | --- | --- | --- |
| Pristine | Intensity / Counts | 3.03×104 | 3.05×104 |
|  | Peak position / eV | 192.41 | 192.41 |
|  | FWHM / eV | 2.05 | 2.048 |
|  | Asymmetry factor | 0.001 | 0.239 |
|  | Residue | 201.2838567 | 197.4717028 |
| 1st charge | Intensity / Counts | 3.24×104 | 3.24×104 |
|  | Peak position / eV | 190.24 | 190.21 |
|  | FWHM / eV | 1.968 | 1.956 |
|  | Asymmetry factor | 0.001 | 0.175 |
|  | Residue | 173.1236171 | 170.7620849 |
| 1st discharge | Intensity / Counts | 3.13×104 | 3.11×104 |
|  | Peak position / eV | 190.55 | 190.53 |
|  | FWHM / eV | 1.99 | 1.975 |
|  | Asymmetry factor | 0.001 | 0.083 |
|  | Residue | 240.825556 | 240.8535978 |

Table S1 Curve fitting results of photoelectron spectra in the B 1s region of LCO-LBO composite electrode.

Figure S7 (a) Co 2p3/2 and (c) B 1s photoelectron spectra of the LCO-LBO composite electrode before and after charge/discharge cycles with calibration using the B 1s peak of LBO at 191.5 eV. (c) Magnified graphs of dashed box shown in (a).