Electronic Supplementary Material

Highly sensitive determination of ammonia nitrogen by nanocubic copper prepared by direct electrochemical deposition

Qianhui LUO a, Yulin ZHENG b, Qing CHANGc, Yuqun XIEb, , Guodong JIANGa,

a  School of Material and Chemical Engineering, Hubei University of Technology,28,Nanli Road,Hong-shan District, Wuhan 430068, China

b  School of bioengineering and Food Science, Hubei University of Technology, 28,Nanli Road,Hong-shan District, Wuhan 430068, China

c College of resources and Environment, South-central Minzu University,182, Minzu Avenue, Hongshan District, Wuhan 430074, China

Corresponding author: E-mail: jianggd@hbut.edu.cn (G. Jiang), Tel: +86 27 59750870

Figure S1. Cyclic voltammogram of bare Pt electrode in 0.9 M H2SO4 solution containing 0.075 M CuSO4.

200 nm

500 nm

2 μm

(e))

(d))

(c)

(b))

(a)

1 μm

200 nm

500 nm

(f))

Figure S2. SEM imagines of nano-Cu electrodes deposited at (a-c) -0.2 V and (e-f) -0.4 V for 60 s.

Figure S3. Linear scan voltammograms of nanocubic copper electrode with different sweep rates ranged from 5 mV/s to 200 mV/s in blank carbonate buffer solution (pH=10). The inset shows the liner fitting plot of the logarithm of the peak current (ip) at -0.03V versus the logarithm of the scan rate (v).