Supporting Information

Effect of Operating Temperature and Additives to Chloroaluminate Ionic Liquid Electrolyte
on Current Efficiency and Surface Morphology of Al Electrodeposit

Koichi UI,a, *, § Ryohei HIBINO,a, §§ Kuniaki SASAKI,b Tatsuya TAKEGUCHI,a, § Tetsuya TSUDA,c, §

Mikito UEDA,d, § Junji NUNOMURA,e, § Yoshihiko KYO,e, § and Yoichi KOJIMA,e, §

a Graduate School of Arts and Science, Iwate University, 4-3-5 Ueda, Morioka, Iwate 020-8551, Japan

b Technical Office for Science and Engineering, Iwate University, 4-3-5 Ueda, Morioka, Iwate 020-8551, Japan

c Faculty of Engineering, Chiba University, 1-33 Yayoi-cho, Inage-ku, Chiba, Chiba 263-8522, Japan

d Faculty of Engineering, Hokkaido University, Kita-13, Nishi-8, Kita-ku, Sapporo, Hokkaido, 060-8628, Japan

e Research & Development Center, UACJ Corporation, 3-1-12 Chitose, Minato-ku, Nagoya, Aichi 455-8670, Japan

*Corresponding Author: kui@iwate-u.ac.jp

§ ECSJ Active Member

§§ ECSJ Student Member

Figure S1. Structural formulas of (a) 1-ethyl-3-methylimidazolium chloride (EMIC)
and (b) 1,10-phenanthroline anhydrate (OP).

Table S1. Orientation coefficient of resulting Al films obtained on the Cu plate substrate from the OP-added bath at 60−100 ℃ and the OP-free bath at 70 ℃.

| Additive | Temperature (℃) | Orientation coefficient |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | 111 | 100 | 110 | 311 |
| OP | 60 | 0.067 | 3.363 | 0.014 | 0.023 |
|  | 70 | 0.016 | 3.438 | 0.006 | 0.007 |
|  | 80 | 0.239 | 2.992 | 0.124 | 0.180 |
|  | 90 | 1.011 | 1.576 | 0.387 | 0.743 |
|  | 100 | 1.338 | 0.922 | 0.623 | 0.923 |
| None | 70 | 0.998 | 1.479 | 0.514 | 0.780 |