Self-assembled cationic surfactant-based electrolytes for rechargeable aqueous zinc metal batteries

Guohong SHEN1, Shinji KONDOU2, §§, Hiroki NAKAGAKI1, Gakuto WADA1, §, Masayoshi WATANABE3, §§§, Kaoru DOKKO1,3, §§，Kazuhide UENO1,3, §§,*

1 Department of Chemistry and Life Science, Yokohama National University, 79-5 Tokiwadai, Hodogaya-ku, Yokohama 240-8501, Japan

2 Department of Materials Engineering Science, Graduate School of Engineering Science, Osaka University, 1-3 Machikaneyama, Toyonaka, Osaka 560-8531, Japan

3 Institute of Advanced Sciences, Yokohama National University，79-5 Tokiwadai, Hodogaya-ku, Yokohama 240-8501, Japan

E-mail: ueno-kazuhide-rc@ynu.ac.jp

§ ECSJ Student Member

§§ ECSJ Active Member

§§§ ECSJ Fellow

Figure S1. (a) 1H and (b) 19F NMR spectrum of CTATFA.

Figure S2. Solubility experiment for choosing suitable anion paired with CTA+.

Figure S3. Contact angel of the aqueous electrolyte droplets, (a) 1 M Li2SO4; (b) 1 M LiTFA; (c) 1 M LiTFA-0.5 M CTATFA on Al foil.

Figure S4. ATR FT-IR spectra of (a) 1 M LiTFA-x M CTATFA (x=0.1-0.5, molar concentration); (b) 1 M Zn(TFA)2-x M CTATFA (x=0.1-0.5, molar concentration).

Figure S5. Shear viscosity as a function of shear rate of (a) 1 M LiTFA-x M CTATFA, (b) 1 M Zn(TFA)2-x M CTATFA and (c) zero shear viscosity for the studied electrolytes as a function of the concentration of CTATFA (x) at 30 °C.

Figure S6. SEM images of Al working electrode after potentiostatic polarization for 20 h at −1.2 V vs. Ag/AgCl: (a) and (b) pristine Al foil; (c) and (d) 1 M LiTFA-0.5 M CTATFA; (e) and (f) 1 M LiTFA.

Figure S7.  SEM images and photographs of Cu electrode after 20 stripping/plating cycles at 1 mA cm−2,1 mAh cm−2 with different electrolytes: (a)-(d) 1 M Zn(TFA)2; (e)-(h) 1 M ZnSO4; (i)-(l) 1 M Zn(TFA)2-0.5 M CTATFA.

Figure S8.  (a)-(c) SEM images and (d) digital image of Cu foil after the initial Zn plating at 1 mA cm−2 and 1 mAh cm−2 using the electrolytes, 1 M ZnSO4.

Figure S9.  XRD pattern of Zn foil before and after stripping/platting over 50 cycles at 1 mA cm-2, 1 mAh cm-2 with different electrolytes.

Figure S10. The charge-discharge curves of Zn/MnO2 cells with 1 M ZnSO4-0.2 M MnSO4, 1 M Zn(TFA)2-0.2 M Mn(TFA)2, and 1 M Zn(TFA)2-0.5 M CTATFA-0.2 M Mn(TFA)2 at a current density of (a)-(c) 0.2 A g⁻¹ and (d)-(f) 0.5 A g⁻¹.