Ionic conduction and electric modulus in Li2S–CaS and CaX2 (X = F, Cl, Br, and I) nanocomposites

Hirotada GAMOa,§, Nguyen Huu Huy PHUCa,†,††,*, Mika IKARIa, Kazuhiro HIKIMAa,§§, Hiroyuki MUTOb, Atsunori MATSUDAa,*,§§

a Department of Electrical and Electronic Information Engineering, Toyohashi University of Technology, 1-1 Hibarigaoka, Tempaku-cho, Toyohashi, Aichi 441-8580, Japan

b Institute of Liberal Arts and Sciences, Toyohashi University of Technology, 1-1 Hibarigaoka, Tempaku-cho, Toyohashi, Aichi 441-8580, Japan

*Corresponding authors: matsuda@ee.tut.ac.jp (A. Matsuda) and nhhphuc@hcmut.edu.vn (N.H.H. Phuc)

† Present address: Faculty of Materials Technology, Ho Chi Minh city University of Technology (HCMUT), 268 Ly Thuong Kiet Str., Dist. 10, Ho Chi Minh City, Vietnam

†† Present address: Vietnam National University Ho Chi Minh City, Linh Trung Ward, Thu Duc Dist., Ho Chi Minh City, Vietnam

§ ECSJ Student Member

§§ ECSJ Active Member

Fig. S1. The Williamson–Hall plots for (a) Li2S and (b) CaS phase in (100−x)Li2S･xCaS.

Fig. S2. SEM-EDS images for (100−x)Li2S･xCaS.

Fig. S3. Conductivity isotherms of Li2S at different temperatures ranging from 130 °C to 170 ℃. The solid lines are the fitting as per Jonscher’s power law, i.e., σ∝ωn at the dispersive regime.

| Table S1. Densities of pellets (d1), theoretical densities (d2), and relative denties (d1/d2) of the (100-x)Li2S-xCaS (x = 10, 20, 30, 50) nanocomposites. d1 was caluculated from the volume measured by the dimensions of the pellet. d2 was caluculated from theoretical densities of an ideal Li2S and CaS crystal phases. |  |
| --- | --- |
| x; d1 (g cm−3); d2 (g cm−3); d1/d2 (%). 0; 1.54; 1.66; 93.0. 10; 1.40; 1.75; 79.6. 20; 1.59; 1.85; 86.3. 30; 1.64; 1.94; 84.5. 50; 1.64; 2.13; 77.4. |

Fig. S4. The imaginary part of modulus M″ versus the frequency of (a) Li2S, (b) 80Li2S･20CaS, (c) 70Li2S･30CaS, and (d) 50Li2S･50CaS at different temperatures.

Fig. S5. A magnified view of the XRD patterns for (a) (100−x)Li2S･xCaF2, (b) (100−x)Li2S･xCaCl2, (c) (100−x)Li2S･xCaBr2, and (d) (100−x)Li2S･xCaI2.

Fig. S6. An Arrhenius plot of the DC conductivities for 80Li2S･20LiI.