Supporting Information for

Stabilizer-free vitamin E nanovehicle for biological research

published in Journal of Oleo Science

Preparations and Characterizations of Stabilizer-free Vitamin E Nanovehicle

Shigesaburo Ogawa*, Katsuya Iuchi, Taro Tsubomura, Kiichiro Totani, and Setsuko Hara

Table of Contents

Page S2

Figure S1. Preparation protocol of dispersion A

Figure S2. TEM image of dispersion A: DL--Toc with phosphotungstic acid staining

Figure S3. Preparation protocol of dispersion B

Page S3

Figure S4. TEM image of dispersion B: DL--Toc with uranyl acetate staining

Figure S5. (a) UV spectra of the chromanol rings in DL--Toc and PMC; (b) Polarity parameter v.s. maximum absorption wavelength, λmax

Page S4

Figure S6. Size dependence of DL--Toc nanoparticles on DL--Toc concentration in the DMSO preparation

Figure S7. UV spectra of ethanol solutions of DL--Toc at different concentrations

Page S5

Figure S8. 1H-NMR spectra of ethanol solutions of DL--Toc at different concentrations

Table S1. Summary of characterizations of the VE dispersions A, prepared using 0.4 wt% ethanol solution and pure water as the water medium

Page S6

Figure S9. (a) Representative UV–vis absorption spectra with and without the DL--Toc dispersion vehicle; (b) A DLS chart after the radical scavenging test

Figure S10. (a) Effect of Tween 80 on UV–vis spectra; (b) representative DLS chart after solublilization in 0.2 wt% Tween 80 aq.

Page S7

Figure S11. Dose-dependence of TBHP on cell viability in %

Figure S1. Preparation protocol of dispersion A.

Figure S2. TEM image of dispersion A: DL--Toc with phosphotungstic acid staining

Figure S3. Preparation protocol of dispersion B

Figure S4. TEM image of dispersion B: DL--Toc with uranyl acetate staining

Figure S5. (a) UV spectra of the chromanol rings in DL--Toc and PMC; (b) Polarity parameter v.s. maximum absorption wavelength, λmax

Figure S6. Size dependence of DL--Toc nanoparticles on DL--Toc concentration in the DMSO preparation

Figure S7. UV spectra of ethanol solutions of DL--Toc at different concentrations

Figure S8. 1H-NMR spectra of ethanol solutions of DL--Toc at different concentrations

Table S1. Summary of characterizations of the VE dispersions A, prepared using 0.4 wt% ethanol solution and pure water as the water medium

| VE | r/nm | PDI |
| --- | --- | --- |
| DL--Toc | 71.8 | 0.13 |
| D--Toc | 74.5 | 0.01 |
| D--Toc | 59.1 | 0.07 |
| D--Toc | 72.2 | 0.05 |
| D--Toc | 47.0 | 0.07 |
| TocToctri | 45.0 | 0.11 |
| Toctri | 67.1 | 0.10 |
| Toc-Q | 52.7 | 0.18 |

Figure S9. (a) Representative UV–vis absorption spectra with and without the DL--Toc dispersion vehicle; (b) A DLS chart after the radical scavenging test

Figure S10. (a) Effect of Tween 80 on UV–vis spectra; (b) representative DLS chart after solublilization in 0.2 wt% Tween 80 aq.

Figure S11. Dose-dependence of TBHP on cell viability in %